## Slide 1
SOL-GEL METHOD USING ETHANOL

## Slide 2
We were forming Ce2Ni205 instead we got CeNi0.102 which was annealed for 4 hours at 5000C below it is an xrd graph showing single phase peaks

## Slide 3
We were forming Ce2Ni205 again by changing temperature condition but instead we got CeNi03 which was annealed for 8 hours at 7000C below it is an xrd graph showing single phase peaks

## Slide 4
We were forming Ce2Co205 and we got CeCo307 which was annealed for 8 hours at 8000C below it is an xrd pattern showing single phase peaks

## Slide 5
SOL-GEL METHOD USING CITRIC ACID

## Slide 6
We were forming Ce2Co205 again which was annealed for 6 hours at 5000C below it is an xrd pattern showing single phase peaks

## Slide 7
We were forming CeNi307 which was annealed for 6 hours at 5000C below it is an xrd pattern showing single phase peaks

## Slide 8
We were forming Ce(Co2Ni)07 which was annealed for 6 hours at 5000C below it is an xrd pattern showing single phase peaks